## Slide 1: ScrollTherm® Thermal Treatment Process for CANDU Ion Exchange Resins
CEtech LLC Consulting, Engineering, and Technology Development – Patents Pending
CEtech LLC

## Slide 2: ScrollTherm Process – CANDU IER Overview
  Purpose of Ion Exchange Resin (IER) treatment
    Gasify the resin polymer structure via non-oxidative pyrolysis (400 to 550˚C gasification) thereby separating and concentrating the resultant non-volatile inorganics (including almost all radionuclides).
    Volume reduction target: >5x (treated resin residues [RR] <1/5th pretreatment IER volume)
    Separate and stabilize 14C, 36Cl, and 129I as water insoluble minerals: 14C as CaCO3, 129I as Ag129I, and 36Cl as Ag36Cl.
    Solidify and dispose of Ca14CO3, Ag129I, and Ag36Cl separately or combined with resin residues.
  Treatment throughput per ScrollTherm unit (STV): up to 6.8 m3/day (240 cuft/day)
  Stabilization options of volume reduced, inorganic, treated resin residues - solidification
      Inorganic: geopolymer or hydraulic cement
      Organic: polyethylene or epoxy encapsulation
CEtech LLC ScrollTherm Process – Patents Pending
2

## Slide 3: Pyrolysis of CANDU IERs - Overview
CEtech LLC ScrollTherm Process – Patents Pending
3

## Slide 4: ScrollTherm – CANDU IER Treatment - Options
  Process Flowsheet 1:
  Separate cation and anion resins hydraulically using water. Store separately for treatment.
  Thermally process cation and anion resins separately in the STV to provide enhanced separation and enriched collection of the following:
    Volatile radionuclides from anion resin treatment will be adsorbed from the STV process gas: 129I as Ag129I, and 36Cl as Ag36Cl in the Ag-Zeolyte Adsorber and 14C as Ca14CO3 in CO2 Adsorber.
    Non-volatile, inorganic Resin Residues (RR) from cation and anion treatment will be removed from the STV/FDB as dry, flowable, particulate solids. RR will contain essentially all radionuclides, except 14C, 129I, and 36Cl.
  Solidify enriched Ca14CO3, Ag129I, and Ag36Cl as one very low volume waste and separately solidify the low volume RR as a second final waste form. Alternatively, combine RR, Ag-Zeolyte Adsorber, and CO2 Adsorber post-treatment particulate wastes and solidify as a low volume, high activity final waste form.
  Scrubber salts - moderate volume: primarily very low activity Na2SO4 or CaSO4 (includes all SOx).
  Notes:
  Anion IERs contain essentially all 14C, 129I, and 36Cl and will pyrolyze without SOx production.
  Alternative ScrollTherm processing options can be implemented with additional final waste form options.
CEtech LLC ScrollTherm Process – Patents Pending
4

## Slide 5
CEtech LLC ScrollTherm Process – Patents Pending
5
  ScrollTherm – Process Flowsheet 1 – CANDU IER

## Slide 6: ScrollTherm - Process Flowsheet 1 – CANDU IERs
  Separate cation and anion IERs. Each IER type will be processed separately.
  Optional: Dry IERs to reduce process gas volume in STV thereby improving 14C, 36Cl, and 129I recovery and separation. Utilize steam heated ScrollTherm unit under vacuum to remove most internal water from IERs.
  Cation IER treatment:
    Bypass CO2 Adsorbers.
    Meter/feed cation IER into STV operating at 400 to 550˚C.
    IERs heat-up to pyrolysis temperatures. Resin polymer and organics will thermally gasify via pyrolysis producing a low-volume, VOC stream that mixes with steam from evaporation of slurry, interstitial, and residual water. SOx is partially volatized from the cation resin sulfonic group at >200˚C.
    Inorganics will form volume-reduced, free-flowing RR solids, which comprises non-volatile carbon from resin pyrolysis and essentially all inorganics and radionuclides on the cation IER (all organics destroyed).
    Process gas (comprising VOCs, steam, SOx, and small amount of H2S) and RR particles are discharged from the STV and are transferred to the downstream DeNOx Barrier Filter (FDB).
CEtech LLC ScrollTherm Process – Patents Pending
6

## Slide 7: ScrollTherm - Process Flowsheet 1 – CANDU IERs
  Anion IER treatment:
    Upon completion of STV treatment of cation IER, realign process gas to flow through CO2 Adsorber.
    Meter/feed anion IERs into STV operating at 400 to 550˚C.
    IERs heat-up to pyrolysis temperatures. Resin polymer and organics will thermally gasify via pyrolysis producing a low-volume, VOC stream that mixes with steam from evaporation of the slurry, interstitial, and residual water. No SOx is produced by pyrolysis of anion IER.
    Inorganics will form volume-reduced, free-flowing RR solids, which comprises non-volatile carbon from resin pyrolysis and essentially all inorganics on the IER (all organics destroyed).
    Process gas (comprising VOCs, steam, 14C as mainly 14CO2, 36Cl, and 129I) and RR particles are discharged from the STV and are transferred to the downstream DeNOx Barrier Filter (FDB).
CEtech LLC ScrollTherm Process – Patents Pending
7

## Slide 8: ScrollTherm - Process Flowsheet 1 – CANDU IERs
  DeNOx Barrier Filter (FDB) separates RR particles from process gas. RR particles are periodically removed from the FDB for subsequent cooling and solidification or encapsulation for disposal (contains essentially all non-volatile radionuclides).
  The Ag-Zeolyte Adsorber and CO2 Adsorbers perform the following functions:
    During anion IER treatment: The Ag-Zeolyte adsorber will adsorb 36Cl as Ag36Cl and 129I as Ag129I from the process gas. The CO2 Adsorbers will adsorb 14CO2 volatized from the treated anion resins as Ca14CO3. The CO2 Adsorbers adsorb no SOx as anion resins contain no sulfur.
    During cation IER treatment: Bypass the CO2 Adsorbers so SOx released from the cation IER sulfonic group decomposition will not be adsorbed. This ensures that the CO2 Adsorbers only remove and convert 14CO2 from the anion resin treatment into Ca14CO3. Periodically remove and replace portion of adsorber bed with fresh calcium adsorbent.
  Process gases are then oxidized in the electrically-heated Thermal Oxidizer (ETO), cooled and scrubbed in the Quencher Scrubber, HEPA filtered, and monitored prior to discharge. ETO will oxidize any H2S in process gas to SOx. Quencher Scrubber will remove SOx from ETO offgas as Na2SO4.
  Optional: Convert Na2SO4 from scrubber system into CaSO4 for solidification and/or disposal.
CEtech LLC ScrollTherm Process – Patents Pending
8

## Slide 9: ScrollTherm Process – Scrubber Solution Disposition Options
    Flowsheet 1
    Option 1: Dry and encapsulate Na2SO4 scrubber salts in polymer and dispose.
    Option 2: Convert water soluble Na2SO4 scrubber salts to water insoluble CaSO4:
      Add Ca(OH)2 to scrubber solution in separate vessel, thereby converting Na2SO4 to water insoluble CaSO4 (gypsum) and NaOH solution,
      Remove precipitated CaSO4 from NaOH solution and rinse CaSO4 solids,
      Dry wet CaSO4 to form CaSO4-1/2H2O (hemi-hydrate, gypsum) and solidify gypsum by adding water (no solidification agent required), then
      Recycle/reuse NaOH solution in Quencher Scrubber.
    Option 3: Solidification using hydraulic cements (problematic, large volume increase)
CEtech LLC ScrollTherm Process – Patents Pending
9

## Slide 10: CEtech LLC
  Please contact CEtech for detailed technical information on ScrollTherm treatment of CANDU ion exchange resins presented herein.
  CEtech LLC
  Brad Mason, P.E.
  Director Technology
  brad.mason.pe@cetech-scrolltherm.com
  +1 (509) 537-6529
  https://www.cetech-scrolltherm.com
10